Silvaco III

These simulations will show the effects related to diffusion processes. Advanced diffusion models will be used to observe the influence of point defects on diffusion of B and P using BJT fabrication as an example.

From examples please select:

- Section 38 Athena: Advanced Diffusion and then go to 38.6 advdifex06.in: Simulation of Phosphorus Predeposition Using PLS Model.

  - Run the program and in TonyPlot analyze the overlayer of the plots.

  - Modify the program by adding one more run at surface concentration equal to solid solubility.

  - Discuss the influence of surface concentration on dopant self diffusion and resulting profiles.

- Section 37 Athena: Diffusion Processes Simulation and then go to 37.7 andfex07.in: Emitter Push Effect.

  - Change the process such that: nitride is replaced by oxide and it remains throughout the whole fabrication (no etching).

  - Deactivate P implantation and replace it by P diffusion while specifying P surface concentration first at c.phos=1.0e20. Use the same diffusion method compress full.cpl.

  - Run the program at 1000°C/30min and then at 1050°C/5min. Save your *.str files.

  - In the next repeat step c  but use c.phos=1.0e21 in your diffusions.

  - Explain your results using menu functions in tony plots.