## Slide 1
ECE 7366
Advanced Process Integration
Introduction
Dr. Wanda Wosik
UH, ECE
Text Book: B. El-Karek, “Silicon Devices and Process Integration”
Slides also include files from VLSI Era by Plummer et al., INTEL, etc.
Spring 2016
MW, 4-5:30pm

## Slide 2: Our Course Process Integration
The objective is to use sequential processes for meet particular requirements for various circuits
ITRS will be our main guiding tool

## Slide 3
Evolution of the Silicon Integrated Circuits since 1960s
Increasing: circuit complexity, packing density, chip size, speed, and reliability
Decreasing: feature size, price per bit, power (delay) product
1960s
1990s
• 1960 and 1990 integrated circuits.
• Progress due to: Feature size reduction - 0.7X/3 years (Moore’s Law).
Increasing chip size - ≈ 16% per year.
“Creativity” in implementing functions.

## Slide 4
45 nm Microprocessor Products
Single Core
6 Core
Dual Core
8 Core
Quad Core
>200 million 45 nm CPUs shipped to date

## Slide 5
Intel

## Slide 6
40+ Years of Moore’s Law at INTEL: From Few to Billions of Transistors
2X transistors
every 2 years
Transistor Count has Doubled Every Two Years

## Slide 7
40+ Years of Moore’s Law at INTEL: From Few to Billions of Transistors
END OF TRADITIONAL SCALING ERA ~ 2003
Lasted ~40 YEARS
2X transistors
every 2 years
Traditional Scaling Era
Ghani, Intel

## Slide 8: Transistor Density
Intel 32 nm transistors provide the tightest gate pitch of any reported 32 nm or 28 nm technology
Ghani, Intel

## Slide 9
22nm

## Slide 12
• The era of “easy” scaling is over. We are now in a period where
technology and device innovations are required. Beyond 2020, new
currently unknown inventions will be required.
Cell dimensions
Atomic dimensions
Device Scaling Over Time
Era of Simple Scaling
Scaling + Innovation
(ITRS)
Invention
~16% increase in complexity each year (now:6.3% for µP, 12% for DRAM)
~13% decrease in feature size each year (now: ~10%)
0.25µm in 1997

## Slide 13: SRAM Cell Size Scaling
32 nm, 0.171 um2
45 nm, 0.346 um2
65 nm, 0.570 um2
Transistor density continues to double every 2 years
Ghani, Intel

## Slide 15
ITRS.net

## Slide 16
G. Marcyk, Intel
1997
1999
2001
2004
2007
2010
2013
2016
2 nodes

## Slide 18
http://www2.imec.be/be_en/research.html

## Slide 19
http://www2.imec.be/be_en/about-imec/infrastructure/cleanrooms.html

## Slide 20
Evolution of the Fabrication Process: The Planar Design of Bipolar Transistors
Implementation of a masking oxide to protect junctions at the Si surface
Boron diffusion
SiO2
Mask
Oxidation possible for Si not good for Ge
Oxidation and outdiffusion
Lithography to open window in SiO2
Phosphorus diffusion through the oxide mask
Beginning of the Silicon Technology and the End of Ge devices
The planar process of Hoerni and Fairchild (1950s)

## Slide 21
Photolithography used for Pattern Formation
Beginning of Integrated Circuits in 1959
Kilby (TI) and Noyce (Fairchild Semiconductors)
• Basic lithography process
which is central to today’s
chip fabrication.
Sensitive to light
Durable in etching

## Slide 22
Alignment of Layers to Fabricate IC Elements
Emitter
Collector
Resistor
Base
Resistor
• Lithographic process allows integration of multiple devices side by side on a wafer.
Bipolar Transistor and resistors made in the base region
Accuracy of placement ~1/4 to 1/3 of the linewidth being printed
Vcc
C
B
E
BJT
0V
Contact to collector
R=L/W•Rs

## Slide 23
NMOS and CMOS Technologies
Enhancement NMOS Depletion NMOS
1970s
NMOS
PMOS
1980s and beyond
Smaller power consumption

## Slide 24: Schematic Cross-Section of Modern CMOS Integrated Circuit with Two Metal Levels
IC is located at the surface of a Si wafer (~500µm thick)
PMOS
NMOS
Via
Interconnect
Silicide
Oxide Isolation
M1
M2
OXIDE
TiN

## Slide 25
• Actual cross-section of a modern
microprocessor chip. Note the
multiple levels of metal and
planarization. (Intel website).
Computer Simulation Tools (TCAD)
•Most of the basic technologies in silicon chip manufacturing can now be simulated.
Simulation is now used for:
• Designing new processes and devices.
• Exploring the limits of semiconductor devices and technology (R&D).
• “Centering” manufacturing processes.
• Solving manufacturing problems (what-if?)

## Slide 26
Modern IC with a Five Level Metallization Scheme.
Planarization

## Slide 29
ITRS.net
This graphic clarifies the ORTC Table 1 relationship to gate length. It illustrates consistency with Interconnect TWG transistor M1 contacted half-pitch (also known as “transistor pitch” or “gate pitch”) versus printed gate length (GLpr) and measurable physical gate length (GLph). This dimension is sometimes compared to critical dimension (CD) for manufacturing process control.
The ITRS does not utilize any single-product “node” designation reference. Flash Poly and DRAM M1 half-pitch are still lithography drivers; however, other product technology trends may be drivers on individual TWG tables.
“Nodes”

## Slide 30
ITRS.net

## Slide 34: Intel Logic Technology Roadmap
45 nm 32 nm 22 nm
Process Name: P1266 P1268 P1270
Products: CPU CPU CPU
1st Production: 2007 2009 2011
Intel 32nm: 2nd generation high-k + metal gate
transistors
Ghani, Intel

## Slide 37
ITRS.net

## Slide 41
The traditional finFET (upper left), a trigate on SOI (upper right), trigate on bulk silicon (lower left) and a pseudo-trigate on SOI (lower right). (Source: Texas Instruments)

## Slide 42
Challenges For The Future
• Having a “roadmap” suggests that the future is well defined and there are
few challenges to making it happen.
• The truth is that there are enormous technical hurdles to actually achieving
the forecasts of the roadmap. Scaling is no longer enough.
• 3 stages for future development:
Materials/process innovations
NOW
Device innovations
IN 5-15 YEARS
Beyond Si CMOS
IN 15 YEARS??
“Technology Performance Boosters”
Invention
???
Gate
Source
Drain
• Spin-based devices
• Molecular devices
• Rapid single flux quantum
• Quantum cellular automata
• Resonant tunneling devices
• Single electron devices
Plummer et al.

## Slide 49
Possible Future Transistor Options
Advanced Channel Materials
- III-V and Ge channel materials
Multi-Gate Fin Transistors
- Non planar architecture
Tunnel Transistors
- New transport mechanism
Each transistor structure has many significant
challenges which will have to be successfully addressed
if it is to become a serious contender to silicon MOSFET
Ghani, Intel

## Slide 52: Transistor Performance
Intel 32 nm transistors provide the highest drive currents of any reported 32 nm or 28 nm technology
Ghani, Intel

## Slide 54
?

## Slide 55
CPU Transistor Count & Power Trend
1.E+03
1.E+04
1.E+05
1.E+06
1.E+07
1.E+08
1.E+09
1.E+10
1970
1980
1990
2000
2010
1.E+03
1.E+04
1.E+05
1.E+06
1.E+07
1.E+08
1.E+09
1.E+10
4004
8080
286
486
TM
Pentium® II CPU
Pentium® 4 CPU
Itanium® 2 CPU
2x increase every
2 years
Penryn QC
Power Dissipation Limited to ~100W
BUT increased transistor count needed
in Multi-Core CPU Era !!!
Ghani, Intel

## Slide 59: Trends in Scaling Si Microeletronics and MEMS

## Slide 60
• 1990 IBM demo of Å scale “lithography”.
• Technology appears to be capable of making structures much smaller than
currently known device limits.
ITRS at http://public.itrs.net
• Assumes that CMOS technology dominates over the entire roadmap.
• 2 year cycle moving to 3 years (scaling + innovation now required).
Trends in Increasing Integration Scale of Circuits Past, Present, and Future ICs

## Slide 61: Fundamental Trends
High Volume Manufacturing | 2004 | 2006 | 2008 | 2010 | 2012 | 2014 | 2016 | 2018
Technology Node (nm) | 90 | 65 | 45 | 32 | 22 | 16 | 11 | 8
Integration Capacity (BT) | 2 | 4 | 8 | 16 | 32 | 64 | 128 | 256
Delay = CV/I scaling | 0.7 | ~0.7 | >0.7 | Delay scaling will slow down |  |  |  | 
Energy/Logic Op scaling | >0.35 | >0.5 | >0.5 | Energy scaling will slow down |  |  |  | 
Bulk Planar CMOS | High Probability Low Probability |  |  |  |  |  |  | 
Alternate, 3G etc | Low Probability High Probability |  |  |  |  |  |  | 
Variability | Medium High Very High |  |  |  |  |  |  | 
ILD (K) | ~3 | <3 | Reduce slowly towards 2-2.5 |  |  |  |  | 
RC Delay | 1 | 1 | 1 | 1 | 1 | 1 | 1 | 1
Metal Layers | 6-7 | 7-8 | 8-9 | 0.5 to 1 layer per generation |  |  |  | 
Source: Shekhar Borkar, Intel Corp.

## Slide 64: Scaling - Yields

## Slide 75
Key Messages / Summary
Intel’s Response to end of “traditional-scaling”:
  Uniaxial Strain (90nm and beyond): 32nm is 4th generation of uniaxial strain at Intel
  HiK + Metal Gate (45nm and beyond at Intel)
Future Novel Transistors:
  New Channel Materials:
  Integrate Ge & III-V on top of Silicon. Many device and material challenges remain
  Multi-Gate Fin Transistors:
  Scaling benefits BUT need to demonstrate effective strain implementation,
  matched parasitic resistance to planar and overcome patterning challenges
  BTBT (Tunnel) Transistors:
  Ultimate transistors may need tunnel injection at ultra-low Vcc. Would need
  new materials with more efficient tunneling and atomic scale fabrication control
Many exciting materials, physics and integration
challenges left to continue CMOS scaling
These innovations have enabled Intel to maintain historical performance gains on recent nodes
Ghani, Intel

## Slide 78
Don’t Forget About MEMS